RICH ECO Series

RICH ECO Series

RICH ECO is a Duct-fresh ink series for sheetfed offset printing made of vegetal oils, phenolic resins ,mineral oil distillates

Technical data

|  |  | LIGHT (IWS) | ALCOHOL | NITRO | ALKALI | VISOSITY | TACK |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | FASTNESS !=POOR 8=EXCELLENT |  |  |  | 30°C, Laray, poises | @800 RPM LLOYEDS , units |
| BGL 5001 | Q/S PROCESS RICH ECO YELLOW | 4 | + | + | _ | 200 - 410 | 10 - 12 |
| BGL 5002 | Q/S PROCESS RICH GOLD MAGENTA | 4 | + | + | _ | 200 - 430 | 10 - 12 |
| BGL 5003 | Q/S PROCESS RICH GOLD CYAN | 8 | + | + | + | 190 - 380 | 11 - 12 |
| BGL 5004 | Q/S PROCESS RICH GOLD BLACK | 8 | + | + | + | 250 - 410 | 11 - 12 |

# *Standard tone, warm

## Product features

| Trapping 5 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Dot sharpness 5 |  |  |  |  |  |  |  |
| Setting 6 |  |  |  |  |  |  |  |
| Oxidative drying 5 |  |  |  |  |  |  |  |
| Gloss@60 degree 38 to 46 |  |  |  |  |  |  |  |
| Rub resistance 5 |  |  |  |  |  |  |  |
| Rapid further processing 5 |  |  |  |  |  |  |  |

Values from 1 (lower range) to 7 (highest range)

## Printing behaviour

- Suitable for printing at high speeds.

- Suited for all types of dampening solutions.

- Excellent water-ink balance.

- Suitable for perfecting presses.

- Duct fresh.

- Applications: edition, commercial and packaging.

## Recommendations:

- Cleaning: it is recommended to clean the rollers at long stops as well as to apply an anti-skin spray in the ink duct.

- Storage: store at temperatures between 20-35 °C. Avoid the direct exposure to light and heat sources. Once the can has been opened, it is recommended to add an anti-drier layer in order to avoid the skin appearance. A well- conditioned and clean work environment ease the good behaviour of all the components during the printing process.

RICH ECO series does not have expiry date at short or medium term.

## RICH ECO series is an exclusive design of the R&D   Department of BLACK GOLD PRINTING INKS

The aim of our technical documents is to inform and advise our customers. The information provided herein is correct to the best of BLACK GOLD PRINTING INKS   knowledge and belief. No liability for any errors, facts or opinions will be accepted. Customers must verify and test by themselves the suitability of this product for their application. No liability for any loss as a result of any person placing reliance on any material contained herein will be accepted.